## Slide 1
The Mallee Bull Discovery and Exploration in the Central Cobar Basin
Michael Oates ,Bob Brown & Nathan Chapman
Mines and Wines 2013
(Image: DDH1 drilling at Mallee Bull)
Peel Mining Limited (ASX:PEX)
Mines and Wines – Sept 2013
www.peelmining.com.au

## Slide 2: Mallee Bull Location
Mallee Bull
Notes: Located in central NSW 110km south of the town of Cobar, 10km east of the Gilgunnia rest stop of the Kidman highway

## Slide 3: Cobar Superbasin (David 2005)
Notes: Mallee Bull is located adjacent the historic four mile goldfield in the central region of the Cobar Super Basin, north of the Walters Range Shelf where the volcanic dominated Rast and Mount Hope troughs appear to coalesce and mix with turbiditic sediments of the Cobar Superbasin. Its proximity to the Wagga to Nymagee lineament

## Slide 4: EL7461 pegged Sept 2009
Notes: Peel mining pegged EL7461 in September 2009 on the basis of the two historic goldfields, geology prospective for “Cobar Style” mineralisation, untested geophysical target and its proximity to the Mayday mine.

## Slide 5: Local Setting
Mallee Bull
No obvious surface expression
Western limb of south plunging anticlinorium
Ore body dips steeply to the west
Mineralisation parallel to sub parallel to bedding
120m wide , up to 20m thick, 700m deep so far
Dominant steep axial plane cleavage
Upright symmetrical folding
West dipping NNW hanging wall fault
NNE Fault associated with fluid movement
Deposition within dilation zones and porous units

## Slide 6: Stratigraphy
Hosted by rocks of the Upper and Lower Amphitheatre gp
Upper Amphitheatre Group - Mallee Bull Formation
Lower Amphitheatre Group – Shume Formation
Allocthonous Strata separate the two
  Mallee Bull Formation Allocthonous Facies
  Shume Formation Allocthonous Facies
Quartz Arenite marks the top of the Shume Formation
  Keep it Dark Sandstone Member

## Slide 7
Shume Formation
Turbiditic sequence
Well Bedded, graded
Fine to medium grained sandstones to mudstones
Abundant dewatering structures
Generally less than 0.5m thick up to 2m
Single well developed cleavage
Similar detrital composition to Mallee bull formation

## Slide 8
Shume Formation in outcrop
Notes: Shume in outcrop

## Slide 9
Shume Formation in core
Graded beds < 2m
Notes: Shume turbidites in core showing graded beds of fine to medium grained sandstones and mudstones, beds up to 2m thick and commonly less than 0.5m.

## Slide 10: Dewatering Structures
Sedimentary Dyke
Disrupted and Rotated beds
Notes: Dewatering structures are common throughout

## Slide 11: Dewatering Structures

## Slide 12: Allocthonous Facies
Felsic Volcaniclastic sandstone beds
Pebbly Sandstone
Diamictite with subordinate bioclastic
(Coarse crinoids, rugose and tabulate corals)
Micritic Limestone

## Slide 13
Allocthonous Facies

## Slide 14
Allocthonous Facies

## Slide 15: Keep it Dark Sandstone
Fine grained, well sorted and massive
Quartz Arenite
Deposition from different province
Cm to 10m thick
Massive quartz-calcite veins
Rare laminated beds
Mass flow margins?

## Slide 16: Keep it Dark Sandstone
Quartz /Calcite Veins
Cm to up to 10m thick
Notes: Keep it Dark sandstone, well sorted, super mature, massive quartz arenite with common white quartz –calcite veins. Ranges in thickness from cm’s to more than 10m and is locally absent. Interpreted as a mass flow deposit sourced from a different providence to that otherwise supplying sediment to the basin.

## Slide 17: Margins of mass flow lobes
Notes: In places it forms thinly laminated and rarely cross laminated bed, probably representing the extreme margins of the mass flow lobe.

## Slide 18: Mallee Bull Formation
Turbiditic sequence
Graded, fine to medium grained sandstones to mudstones
Dewatering structures
Generally less than 0.5m thick
Similar detrital composition to Shume

## Slide 19: Mallee Bull Formation

## Slide 20: Mineralisation
Mineralisation is essentially stratabound and hosted by turbiditic sedimentary rocks with significant allocthonous felsic volcanics and limestone
Mineralisation occurs as massive sulphide lenses, broad disseminations and a copper-rich stringer zone
Mineralisation surrounded by pyrrhotite halo giving magnetic signature
Significant mineralisation occurs stratigraphically below Keep it Dark Sandstone

## Slide 21: MINERALISATION AND STRATIGRAPHY

## Slide 22: 3D Flythrough

## Slide 23: MINERALISATION AND STRATIGRAPHY

## Slide 24: MINERALISATION AND STRATIGRAPHY

## Slide 25: Mineralisation Types
1) Disseminated and Joint Fill Pyrite
2) Disseminated Pyrrhotite
3) Massive to Semi Massive Sulphide Lenses
4) Disseminated Mixed Sulphides
5) Cupriferous Stringer Zone

## Slide 26: 1) Disseminated and Joint –Fill Pyrite
Notes: Framboidal pyrite showing preference for sandstone laminations

## Slide 27: 2) Disseminated Pyrrhotite

## Slide 28: 3) Massive to Semi Massive Sulphides
- massive and replacement textured Pyrite and Pyrrhotite
- Single or multiple stacked lenses up to 10m
- minor to trace chalcopyrite, arsenopyrite, sphalerite, galena, rare cassiterite
- anomalous Cu-Pb-Zn-Au-Ag-As
- sharp to gradational boundaries
- locally grade into stringer or disseminated styles
Notes: Point 3 in abstract

## Slide 29: Massive to Semi Massive Sulphides

## Slide 30: Massive to Semi Massive Sulphides

## Slide 31: Massive to Semi Massive Sulphides

## Slide 32: 4) Disseminated Mixed Sulphides
- bedding and clast replacement aggregates of pyrrhotite, sphalerite, galena, minor pyrite, chalcopyrite
- anomalous Pb-Zn-Cu-Ag-As
- locally mass together to form stringer veins or semi-massive aggregates
-laterally equivelant to and associated with massive sulphide lenses
Notes: Point 4 in abstract

## Slide 33: Disseminated Mixed Sulphides

## Slide 34: Disseminated Mixed Sulphides
Local semi massive aggregates of coarse inetermixed sphalerite and galena

## Slide 35: Disseminated Mixed Sulphides

## Slide 36: 5) Cupriferous Stringer Zone
- pyrrhotite, chalcopyrite, trace to minor arsenopyrite, galena, sphalerite, cassiterite, boulangerite, gold
- anomalous Cu, Ag, Au (in breccia zones), minor Pb
- stringer veins locally aggregate to form semi-massive and massive bodies
- local quartz-sulphide breccias associated with anomalous Au
- local disseminated chalcopyrite
Notes: Point 5 in the abstract

## Slide 37: Cupriferous Stringer Zone

## Slide 38: Cupriferous Stringer Zone
Flow laminae from deformation and remobilisation

## Slide 39: Cupriferous Stringer Zone

## Slide 40: Cupriferous Stringer Zone
Quartz healed jigsaw breccia

## Slide 41
Alteration
sericite alteration of feldspars and ferromagnesium minerals altered to black (Mg)chlorite

## Slide 42: Silicification and black chlorite

## Slide 43: Exploration History
Discovered in 1895 producing 660g

## Slide 44: Testing the bulk mining potential of the gold workings
RAB and Auger drilling, mapping, rock chip sampling, trenching
Gold restricted to two Quartz types throughout gold fields
Bucky quartz – Au, poor in base metals, pale green chlorite
Laminated quartz, commonly folded – Au + Cu/Pb/As/Zn signature
cm to meter thick
Strike 020, 120 or 150 and thought to be exploiting foliation
1970 Milstern Exploration/Mount Hope Minerals
1974 Penzoil of Australia
1988 Epoch Mining
1996 Renison Ltd

## Slide 45: 1976 Union Corporation
Union corportion

## Slide 46: 1976 Union Corporation

## Slide 47: Newmont 1984
David, 2005

## Slide 48: EL7461 pegged as open ground Sept 2009
Local rocks age equivalent to Cobar host
Untested magnetic anomalies
8 kmE of May Day Au-Ag-Pb-Zn-Cu deposit
Deep water and shallow water sediments
Adjacent historic workings
Favourable trap site – nose of anticline
High strain zone

## Slide 49: Peel Mining VTEM survey December 2010
Notes: Coincident magnetic anomaly and discrete late time EM conductor

## Slide 50: 3 Rounds of Drilling before Success
First round of drilling was RAB down to 60m over anomalies
Second round of RC drilling encouraging
DHEM, FLEM and Gyroscopic surveys of drill holes
Third round of drilling success

## Slide 51
For more information:
Rob Tyson
Managing Director
rtyson@peelmining.com.au
Unit 1, 34 Kings Park Road,
West Perth, WA 6005
Tel: 08 9382 3955
Peel Mining Limited (ASX:PEX)
www.peelmining.com.au